APPLICATION NOTES FOR USING RIVALE FAST GLASS AND MAX GLASS TWO COMPONENT VARNISHES ON TEAK

# Products

## Manufacturer’s Technical Data for FastGlass

| Type of Product | Two-Component Varnish |
| --- | --- |
| Mixing Ratio by Volume | (2l) Mix 2 Parts Sol. A with 1 Part of Sol. B |
| Colour | Clear |
| Dust Free (at 20°C/68°F) | After 15 - 20 minutes |
| Recoat Time (at 2O°C/68°F) | After 6 - 8 hours |
| Specific Gravity | 1 liter = Kg. 1.05 * 0.01 |
| Viscosity | 40 - 50 sec. (Ford Cup 04 at 20°C/68°F) |
| % Non-Volatile | 53+/- 1 |
| Theoretical Coverage | 108 sq. ft./Liter for 40 dry microns |
| Pot Life (at 20°C/68°F) | 4 - 5 Hours |
| Packaging | 1.5 liter Kits (6 Kits per case) |

## Technical Data for MaxGlass

| Type of Product | Two-Component Varnish |
| --- | --- |
| Mixing Ratio by Volume | (2l) Mix 2 Parts Sol. A with 1 Part of Sol. B |
| Colour | Clear |
| Dust Free (at 20°C/68°F) | After 30-40 minutes |
| Recoat Time (at 2O°C/68°F) | After 6 - 8 hours1 |
| Specific Gravity |  |
| Viscosity |  |
| % Non-Volatile |  |
| Theoretical Coverage |  |
| Pot Life (at 20°C/68°F) |  |
| Packaging | 1.5 liter Kits (6 Kits per case) |

## Thinners

Thinner 871 for hot or windy conditions

Thinner 817 for normal conditions.

## Distributor

Rivale Yacht Systems

97 Cove Street

New Bedford, MA 02744
Tel. (800) 938-3343

Fax (508) 984 – 0012

http://www.rivale.com/

## Suppliers

Cyber Marine:			  http://www.cyber-marine.com/bridges/rivale.html

Fisheries Supply Co.	1-800-426-6930

1900 N. Northlake Way #10 	http://www.fisheries-supply.com/

Seattle, WA 98103 	e-mail:mail@fisheries-supply.com

# Application Notes for Teak

## Teak

Teak is an oily, grainy, and porous wood that does not easily take to varnish.  It must be properly sealed before varnishing.  These notes are for a brushed applictation.  The application is done in three steps over 4 or more days:

- Day 1: 2 seal coats

- Days 2 & 3: 8 build coats

- Day 4: 3 finish coats

## Sealing – 2 Coats

MaxGlass is used for sealing as it is more flexible, has less solids and penetrates better.  It fills the grain. Apply two coats with a 1 hour recoat time.  The procedure is as follows:

- Coarse sand the teak with 80 grit sandpaper.

- Use MEK or Acetone to wipe down.  The brown oils will come out of the wood.  Repeat this 4 or 5 times until the oils stop showing up on the rag.

- Thin MaxGlass 60% to 100% with 871 (slow thinner) for first seal coat application.

- Thin MaxGlass 60% with 871 (slow thinner) for second seal coat application.  Wait about 2 hours for the second seal coat.

- Bubbles may show on the surface from internal outgassing.

- Let dry and sand with 180 grit.  Remove all dust using tack cloths.

- Change any masking tape.

## FastGlass 2-Component High-Build Varnish – 8 Coats

FastGlass has higher solids and dries faster.  The point of FastGlass is to build up a base which is sanded back to a perfectly flat and smooth surface.  This is done over two days, applying 4 coats per day.  Heavy sanding at the end of both days produces the nice, smooth base to which the UV topcoat is applied.  It is unfortunate to sand away so much of this expensive product, but that is its purpose.  The application procedure is as follows.

- Thin 10-20% with appropriate thinner depending on weather and wind conditions.

- Recoat as soon as it is touch dry.  Add thinner as necessary to keep the consistency constant.

- Do 4 coats in one day.

- Sand with 220 grit after 4 coats have been applied.

- Change any masking tape.

- Add 4 more coats the next day.  Make sure to remove all dust with tack cloths before re-coating.

- Sand with 220.  Nice and smooth.  Remove all dust using tack cloths.

## MaxGlass 2-Component UV Varnish – 3 Coats

MaxGlass provides the UV protection.  It is more flexible and durable than the FastGlass.  It dries faster for a mirror finish.  MaxGlass is applied annually over previously finished work to maintain the varnish coating (use 2 coats/yr for this purpose).  The application procedure is as follows.

- Make sure surface is clean, dry, dust-free.

- Thin 10-20% with appropriate thinner depending on weather and wind conditions.

- Apply 2 coats.  MaxGlass should  be touch dry in 30 minutes.  Recoat at touch-dry + 30 minutes.

- Light sand with 320.  Remove all dust using tack cloths.  Probably will not need to re-tape.

- Apply final coat.  Thin product 25%.

## General Notes

  - MaxGlass and FastGlass are remarkably forgiving of temperature, wind, and humidity – far more than many other products.  However it is best to apply your final coat at least 1 hour before sundown.

  - Mix the two-part varnigh together first, the add thinner and mix thoroughly.  Failure to mix any 2-part compound can result in undesirable results.  We have had “fish-eyes” result from poor mixing.

  - Make sure temperature of all ingredients is the same.  It is best to let the Rivale equilibrate to room temperature before use.

  - Note that if the day is very hot use the less volatile thinner, #817.

  - This product seems to work best above 65F.

Note:  In practice we recoat MUCH sooner than this.  See notes below

Careful with MEK and acetone as well as with the Rivale itself.  Use a proper solvent mask.

3M Blue tape is recommended.  Never use the beige stuff.